**DIXON CORRECTIONAL EPOXY OF GYM FLOOR**

**Scope of Work:**

The Contractor shall provide all labor, materials, equipment and tools in order to prep and apply Epoxy to approximately 2,000 square feet of existing concrete gym floor. All work shall be performed during normal business hours: 7:00 AM – 3:30 PM Monday-Friday.

A mandatory job-site visit is required to inspect location the job will be performed

Agency contact: Will Bunch

 225-634-6101

**Location:**

Dixon Correctional Institute

5568 Highway 68

Jackson, LA 70748

**Specifications:**

**Project Location: Gymnasium**

1. The Contractor shall remove any old paint on the concrete with a large concrete grinder with dust extraction, and repair any cracks and spalls.
2. The Contractor shall apply primer/sealer, ProRez ProPoxy Moisture Blok (MB) or equal, 100% solids epoxy primers to seal substrate.

**Specify Brand/Model of Epoxy Primer Bidding: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_**

1. The Contractor shall scrape and vacuum surface for any loose Moisture Blok and flakes. The Contractor shall then apply base coat, ProRez ProPoxy (S) or equal, epoxy in clear. Flakes shall be included in this layer. Flakes shall be ProRez PF 200 or equal using double broadcast method, specially blended polymer flakes (macro ¼ “).

**Specify Brand/Model of Clear Epoxy Bidding: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_**

**Specify Brand/Model of Flakes Bidding: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_**

1. The Contractor shall scrape, vacuum any loose ProRez Propoxy Standard (S) or equal.
2. The Contractor shall apply finish coat ProRez ProThane Standard (S) or equal, ultra-high solids, high performance urethane topcoat in satin finish.

**Specify Brand/Model of Topcoat Bidding: \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_**

1. Flooring colors shall be F9908 Canary Yellow, F5910 JD green, and F1050 Black (or equal).

**Other requirements**:

1. A one year warranty shall be provided by the Contractor for all work.
2. Work shall be performed Monday-Friday from 7:00 am – 3:30 pm. The Contractor shall contact Facility Maintenance Coordinator Will Bunch @ 225-634-6101 to schedule.
3. The Contractor’s representatives are subject to a search of their vehicles, possessions and persons. This is necessary to preclude the introduction of weapons, ammunition, explosives, cell phones, alcohol, escape devices, drugs and drug paraphernalia or other forbidden items or contraband into the prison environment. All searches of visitors shall be conducted in accordance with Department Regulation No. C-02-005 and Penitentiary Directive No. 09.004 and 09.004A.
4. The Contractor’s representatives shall follow all institutional policies and procedures while performing work on facility grounds.
5. The Contractor shall be subject to a conference/training with facility staff after the contract is executed and before performing any work.