## RFx  3000026590

## Contract Title: Aggregates – LDWF

## Attachment B - Specifications

Rock 1

Specification Gradation for #610 Limestone

Gradation Sieve Size                      	 % 		Passing

1-1/2" (37.5 MM)                       		100  		100

1”        (25.0 MM)                       		 85  		100

1/2"     (12.5 MM)                      	  	 40  		 75

#4      (4.75 MM)                        		 15   		 40

Moisture  = Sensity Data          (ASTM D 698-C)

Maximum Density   …………………134.8

Optimum Moisture  ………………….    7.7

Los Angeles Abrasion    (ASTM C 131 AASHTO T-96)

Grading………………………………… A

% Loss    ……………………………… 29

Flat & Elongated     (ASTM D 4791)     0.0

Unit Weight  - Lbs. Per Cubic Foot   (ASTM C 29 AASHTO T-19)

Dry Loose ………………………….. 100.0

Dry Rodded ………………………..  111.0

Sodium Sulfate Soundness   (ASTM C 88 AASHTO T-104)

% Loss …………………………….    9.0

Plasticity Index   (ASTM D 4318)       0.0

Liquid Limit                              	      16.3

Plastic Limit                              	      0.0

Rock 2

Specification Gradation for #57 Limestone

Gradation Sieve Size                          %  Passing

1-1/2" (37.5 MM)                               100 100

1"      (25.0 MM)                                 95  100

1/2"    (12.5 MM)                                25   60

#4      (4.75 MM)                                  0   10

#8      (2.36 MM)                                  0    5

Specific Gravity   (ASTM C 127  AASHTO T-85)

Bulk Dry……………………………… 2.64

Saturated Surface Dry …………….. 2.67

Apparent …………………………….. 2.71

Absorption ……………………………1.00

Los Angeles Abrasion    (ASTM C 131  AASHTO T-96)

Grading ………………………………A

% Loss …………………………….. 27.00

Unit Weight - Lbs. Per Cubic Foot   (ASTM C 29   AASHTO T-19)

Dry Loose ………………………… 81.00

Dry Rodded ………………………. 92.00

Sodium Sulfate Soundness            (ASTM C 88  AASHTO  T-104)

% Loss ……………………………  3.50

Rock 3

Specification Gradation for Coarse Aggregate

No. 1 Limestone (1.5" X 3")

Gradation Sieve Size                     	 % 	Passing

4"   	 (100 MM)                       		100 	100

3-1/2"   (90  MM)                    	    	90 	100

3"         (75  MM)                       		 - 	 -

2-1/2"  (63  MM)                        	           25 	 60

1-1/2"   (37.5MM)                      	   	0  	 15

3/4"      (19  MM)                       	           0   	   5

Typical Gradation Sieve                                      Passing

4"       	(100 MM)                          		            100

3-1/2"   (90 MM)                          		             95

3"      	 (75 MM)                          			  91

2-1/2"   (63 MM)                         			  40

1-1/2"   (37.5MM)                      		   	  10

3/4"    	 (19 MM)                      			    1

Specific Gravity (ASTM C 127  AASHTO T-85)

Bulk Dry  …………………………………… …..………    2.64

Saturated Surface Dry ……………………… …………...2.66

Apparent …………………………………. ………………..2.70

Absorption ………………………….. ……………………  .90

Los Angeles Abrasion               (ASTM C 131  AASHTO T-96)

Grading ……………………………….. …………………….. A

% Loss  ……………………………… …………………….. 29.00

Unit Weight  - Lbs. Per Cubic Foot  (ASTM C29  AASHTO T-19)

Dry Loose ……………………………………… ………………84.00

Dry Rodded……………………………………. ……………… 93.00

Sodium Sulfate Soundness                (ASTM C 88 AASHTO T-104)

% Loss ………………………………………. ………………………. 1.00

Rock 4

Specification Gradation For Sand/Clay/Gravel Aggregation (Pit Run)

Metal Content: 30% minimum with ¼” minimum aggregate size. Aggregates below ¼” in diameter will not count toward total metal.

Fine Particles: Considered as all sand, clay, other soil types, and aggregates below 1/4” shall be of a nature and property that sets up quickly after being spread to form a hard, water-shedding road surface that is not slick. In addition, the material must remain firm and exhibit minimal tendency to for ruts after normal rainfall events. This quality to be determined by LDWF personnel by visual inspection and/or application of water to a freshly spread material.

Rock 5

Fill Dirt

Defined as: 60/40 Clay/Sand/Dirt with Plasticity of 19

Rock 6

#2 Washed Gravel Specifications

- Size Range: Generally 1 ½  to 2 ½ inches (ASTM C33).

- Gradation (ASTM C33): 90%-100% passing 2½-inch, 35%-70% passing 2-inch, 0%-15% passing 1½-inch, 0%-5% passing 3/4-inch.